## Slide 1
Hometown: Kayenta, Arizona
(Navajo: Tó Dínéeshzheeʼ)
Alastair Big Luna (AL)

## Slide 2: Advanced Temperature and Stress Measurements using Optical Fibers

## Slide 3
Section 1
Discussion on how optical fibers work
Discussion on Rayleigh backscatter
Discussion on OFDR
Discussion on the temperature and strain algorithm
Section 2
Characteristics of the LUNA ODiSI-B and temperature data
Research on coupled temperature and strain on the surface of a simulated fuel rod.
Presentation Outline

## Slide 4: Section 1: Background
Optic fibers, Rayleigh scattering, OFDR, Temperature & Strain Algothrim

## Slide 5
Optical fibers may be used for temperature, strain, pressure.
The spatial resolution is very high. Choice of having 1.25 [mm] at 24 [Hz] or 5 [mm] at 100 [Hz] of spacing between each data point.
  For example, in a one-meter sensor, you can have as much 800 points of data for each time step. At 24 [Hz], you have 19,200 points of data for each second.
Fibers are small, nonconductive, noncorrosive, and immune to electromagnetic interference
For these reasons, fiber optic sensors are candidates for research, big data collection for machine learning algorithms, and health monitoring of critical components in power plants or facilities.
Why use fiber optic sensors
Figure: Fiber-optic temperature and strain sensor – 1 [m] length

## Slide 6: Required components for temperature and strain measurements
Single mode fibers
Tunable laser and reflectometer
Temperature and Strain algorithm

## Slide 7
Snell’s law
The critical angle
The bigger the difference between the indices of refraction in the two optical materials, the larger the critical angle.
Optical Fiber Theory – Total Internal Reflection
Figure: Illustration of Total Internal Reflection [1]
[1] https://images.fineartamerica.com/images-medium-large-5/refraction-and-total-internal-reflection-russell-kightley.jpg
[2] https://www.youtube.com/watch?v=N_kA8EpCUQo
Figure: Illustration of Corning Single Mode Fiber (SMF-28 Ultra) [2]

## Slide 8
Outside Vapor Deposition (OVD) process is commonly used in the manufacturing of optical fibers.
3 steps: Laydown, consolidation, and draw.
  Laydown process - a soot preform is made from ultra pure vapors as they react in the flame to form fine soot particles of silica or Germania.
  Consolidation process – the bait rod is removed and the preform is placed in a furnace. The preform is sintered into a solid glass.
  Draw process – the preform is placed in a draw tower and drawn into one continuous strand of silica fiber.
Silica Optical Fiber – Manufacturing process
Figure: Illustration of Laydown process [3]
[3] P. Aithal and H. Ravindra, Textbook of Engineering Physics, 1st ed. Acme Learning Private Limited, 2021.

## Slide 9
First proposed for measuring losses inside single-mode optical fiber system. [3]
Relies on a scan of the Rayleigh backscatter amplitude.
A frequency scan is made by changing the wavelength of the laser and a detector measures the backscatter amplitude
Optical Frequency Domain Reflectometry
Figure 5: Fiber-optic temperature and strain sensor
[4]W. Eickhoff and R. Ulrich, "Optical frequency domain reflectometry in single‐mode fiber", Applied Physics Letters, vol. 39, no. 9, pp. 693-695, 1981. Available: 10.1063/1.92872

## Slide 10
First proposed for measuring losses inside single-mode optical fiber system. [3]
Relies on a scan of the Rayleigh backscatter amplitude.
A frequency scan is made by changing the wavelength of the laser and a detector measures the backscatter amplitude
Optical Frequency Domain Reflectometry
Figure 5: Fiber-optic temperature and strain sensor
[4]W. Eickhoff and R. Ulrich, "Optical frequency domain reflectometry in single‐mode fiber", Applied Physics Letters, vol. 39, no. 9, pp. 693-695, 1981. Available: 10.1063/1.92872

## Slide 11: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735 [Accessed 30 July 2020].
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
I
ω

## Slide 12: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735 [Accessed 30 July 2020].
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
X
I
xm

## Slide 13: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
X
I
Gage length
xm

## Slide 14: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
ω
I
xm

## Slide 15: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
Sample
ω
ω
I
I
xm

## Slide 16: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
Sample
Cross Correlated
ω
ω
I
I
Δω
Δωm
xm
I

## Slide 17: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
Sample
Cross Correlated
Peak Correlated to a specific location
ω
ω
I
I
Δω
Δωm
xm
xm
Δωm
X
Δω
I

## Slide 18: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
Sample
Cross Correlated
Peak Correlated to a specific location
ω
ω
I
I
Δω
Δωm
xm
xm
Δωm
X
Δω
I

## Slide 19: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
Sample
Cross Correlated
Peak Correlated to a specific location
ω
ω
I
I
Δω
Δωm
xm
xm
Δωm
X
Δω
I

## Slide 20: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
Sample
Cross Correlated
Peak Correlated to a specific location
ω
ω
I
I
Δω
Δωm
xm
xm
Δωm
X
Δω
I

## Slide 21: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
Sample
Cross Correlated
Peak Correlated to a specific location
ω
ω
I
I
Δω
Δωm
xm
xm
Δωm
X
Δω
I

## Slide 22: Optical Frequency Domain Reflectometry (OFDR)-Algorithm
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015
FFT
I
ω
FFT
X
I
Gage length
Reference
Sample
Cross Correlated
Peak Correlated to a specific location
ω
ω
I
I
Δω
Δωm
xm
xm
Δωm
X
Δω
I

## Slide 23: Frequency Shift correlated to Temperature
Temperature Correlation for the ODiSI-6104
Interrogator using OFS ClearLite POLY 1310 21 NA. Temperature range: 17 [C] to 800 [C]

## Slide 24: Section 2 Distributed Temperature Sensing
LUNA ODiSI-B and ODiSI-6000

## Slide 25
High Temperature Characteristics of the LUNA ODiSI-B and SMF

## Slide 26
High Temperature Characteristics of the LUNA ODiSI-B and SMF in Air

## Slide 27
SMF modifications to withstand High Temperature Environments
Test Parameters | 750 [C] - HE | 750 [C] - BN
Interrogator System | Luna ODiSI-B | Luna ODiSI-B
Type of Optical Fiber | Single mode (SMF-28e) | Single mode (SMF-28e)
Heater Type | Tube Furnace | Tube Furnace
Anneal Type | 800 [C] for 2 [hrs] | 800 [C] for 2 [hrs]
Typical Experimental Timeframes | Until failure | Until failure
Termination End Types | ~30 degree polish | ~30 degree polish
Backfilled Gas Type | Helium | Air with Boron Nitride coating
Optical Fiber Coating | Mechanically Removed | Mechanically Removed

## Slide 28: Optical fiber temperature sensors survivability test in 750 [C] furnace
Plot shows the signal loss for the initial keys of Helium fiber (magenta) and BN fiber (blue). Red line shows 50% signal loss threshold. Helium and BN exceeded the 50% line at 18.6 [hr] and 42.4 [hr], respectively.
Corning SMF-28 Ultra can survive 750 [C] temperatures for 1780 hours (10.6 weeks) when protected with Helium gas cover or Boron Nitride coating
If we consider a 50% signal threshold for both He and BN fibers as a metric, then this test shows BN helps the fiber maintain signal more than the Helium backfilled gas by about 24 hours.
31 reference keys were made for both the Helium fiber and BN fiber. Creating numerous reference keys is not ideal to maintain signal, and therefore, we are searching for fibers that have enhanced Rayleigh scatter signals.
18.6 [hrs] – He
42.4 [hrs] – BN

## Slide 29: Changing Reference Keys to increase sensitivity and signal
Rekey
At 700[C]

## Slide 30
UW-Madison’s high pressure testing loop can simulate PWR conditions using single or multiple heating rods.
PWR conditions can reach temperatures up to 400 [C] and pressures up to 25 [MPa].
Fiber optic sensor (FOS) system used to capture distributed temperature measurements with spatial resolution ranging from 1.25 [mm] to 5 [mm].
Critical Heat Flux (CHF) events detected, and trigger shut down of experiment to protect heat rod and testing facility.
Health Monitoring via Distributed Temperature Measurements
Figure: (a) High pressure testing loop. (b) Experimental temperature profile [C] mapped on Position [m] vs Time [s] plot. White spots represent no data. (c) Temperature [C] vs Position plot [m] of CHF event.

## Slide 31: Distributed Strain Sensing
LUNA ODiSI-B

## Slide 32
Temperature and Strain FOSs are wrapped and bonded around tubes in a helical trench. The helical configuration allows for the FOSs to be decomposed into its axial and circumferential components.
Develop a methodology for collecting strain data in high-temperature and high-pressure environments. The temperature comp The strain data needs to be compensated for temperature influence.
Changes in the reflected spectrum due to strain or temperature are analogous to the spectral shift of a Bragg grating:
Health Monitoring via Distributed Strain Measurements
Figure: Schematic of helical trench pairs on a 3/8 [in] O.D. tube

## Slide 33: Experimental Setup
Nitrogen cylinder. (1)
Lindberg tube furnace 1200 [C] max. (2)
1” OD SS304 Tube (3)
ODiSI-B & ODiSI-6104 modules (4)
Testing article (5)
Fiber Sensors (6)
Thermocouples (7)
(1)
(2)
(3)
(4)
(5)
(6)
(7)

## Slide 34: Embedded Temperature and Strain FOS
½” O.D. x 0.5” SS tube for holding 0.030” O.D. SS Capillary tubes
0.030” O.D. SS Capillary tubes
Embedded Strain FOS (top)
Temperature FOS (bottom)

## Slide 35: Isothermal Plots
The addition of the 4 thermocouples shows the fiber data is providing good temperature data.
Also assures isothermal conditions.

## Slide 36: Isothermal Plots
TFOS
SFOS
_
Fig. Plot showing the Frequency Shift (GHz) response as function of the fiber length for 300°C. The shaded area represents the embedded fibers
Fig. Plot showing the corrected Frequency Shift (GHz) data for the embedded strain fiber.

## Slide 37: Plots for 100 [C]
Chart: Mechanic Strain at 100 [C]
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400 | 1500
MECHANICAL 1 | -197.1177 | -198.4668 | -199.7762 | -200.8522 | -201.8147 | -202.7451 | -203.4463 | -203.0236 | -204.6418
MECHANICAL 2 | -197.2498 | -198.6074 | -199.9613 | -201.0151 | -201.2903 | -203.2398 | -203.543 | -203.0844 | -204.683
MECHANICAL 3 | -197.5331 | -198.9284 | -200.2574 | -201.3088 | -202.3206 | -203.1827 | -203.8877 | -203.3765 | -204.9934
Chart: Isolated Pressure Data at 100 [C]
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400 | 1500
PRESSURE 1 | 0 | -1.3491 | -2.6585 | -3.7345 | -4.697 | -5.6274 | -6.3285 | -5.9059 | -7.524
PRESSURE 2 | 0 | -1.3576 | -2.7115 | -3.7653 | -4.0405 | -5.99 | -6.2932 | -5.8346 | -7.4332
PRESSURE 3 | 0 | -1.3952 | -2.7242 | -3.7757 | -4.7875 | -5.6496 | -6.3546 | -5.8433 | -7.4602

## Slide 38: Plots for 200 [C]
Chart: Mechanic Strain at 200 [C]
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400 | 1500
MECHANICAL 1 | -445.081 | -446.8344 | -446.3191 | -449.6919 | -450.7745 | -451.8744 | -452.6865 | -453.892 | -453.5927
MECHANICAL 2 | -445.4128 | -447.1227 | -446.6176 | -449.9679 | -450.9951 | -452.0177 | -452.8464 | -453.9336 | -453.6366
MECHANICAL 3 | -445.1081 | -446.8492 | -446.3386 | -449.6653 | -450.7142 | -451.7827 | -452.549 | -453.6848 | -453.3639
PREVIOUS RUN-MECHANICAL | -444.4243 | -446.5172 | -448.8371 | -450.5305 | -452.2658 | -453.7314 | -454.8001 | -456.1108 | -456.5557
Chart: Isolated Pressure Data at 200 [C]
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400 | 1500
PRESSURE 1 | 0 | -1.7534 | -1.2381 | -4.6109 | -5.6935 | -6.7934 | -7.6055 | -8.811 | -8.5117
PRESSURE 2 | 0 | -1.71 | -1.2049 | -4.5552 | -5.5824 | -6.605 | -7.4337 | -8.5208 | -8.2238
PRESSURE 3 | 0 | -1.7411 | -1.2306 | -4.5572 | -5.6062 | -6.6746 | -7.4409 | -8.5767 | -8.2558
PREVIOUS RUN-PRESSURE | 0 | -2.0929 | -4.4127 | -6.1061 | -7.8414 | -9.3071 | -10.3758 | -11.6865 | -12.1313

## Slide 39: Plots for 300 [C]
Chart: Mechanical Strain at 300 [C]
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400 | 1500
MECHANICAL 1 | -717.6285 | -719.0994 | -720.4267 | -721.345 | -722.1554 | -722.8567 | -723.1932 | -723.9524 | -723.8506
MECHANICAL 2 | -718.2486 | -719.6074 | -720.8837 | -721.7266 | -722.4353 | -723.4162 | -724.0487 | -723.9361
MECHANICAL 3 | -715.5283 | -716.9872 | -718.2828 | -719.146 | -719.9071 | -720.5574 | -720.9055 | -721.6434 | -721.514
Chart: Isolated Pressure Data at 300 [C]
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400 | 1500
PRESSURE 1 | 0 | -1.4709 | -2.7982 | -3.7165 | -4.5269 | -5.2282 | -5.5647 | -6.3239 | -6.2221
PRESSURE 2 | 0 | -1.3588 | -2.6351 | -3.478 | -4.1867 | -5.1676 | -5.8001 | -5.6875
PRESSURE 3 | 0 | -1.459 | -2.7546 | -3.6177 | -4.3789 | -5.0292 | -5.3773 | -6.1151 | -5.9857

## Slide 40: Plots for 400 [C]
Chart: Mechanical Strain at 400 [C]
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400 | 1500
MECHANICAL 1 | -992.4185 | -994.0481 | -995.602 | -996.7474 | -996.8276 | -998.3236 | -999.1125 | -999.7957 | -999.7279
MECHANICAL 2 | -993.9128 | -995.3142 | -996.7027 | -997.7704 | -998.5218 | -999.1481 | -999.9565 | -1000.5607 | -1000.0604
MECHANICAL 4 | -990.8624 | -992.3159 | -993.7868 | -994.79 | -995.5392 | -996.2553 | -997.0026 | -997.5364 | -997.5737
Chart: Isolated Pressure at 400 [C]
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400 | 1500
PRESSURE 1 | 0 | -1.6296 | -3.1835 | -4.3288 | -4.4091 | -5.9051 | -6.694 | -7.3772 | -7.3094
PRESSURE 2 | 0 | -1.4014 | -2.7898 | -3.8575 | -4.609 | -5.2353 | -6.0436 | -6.6479 | -6.1475
PRESSURE 4 | 0 | -1.4535 | -2.9244 | -3.9276 | -4.6769 | -5.3929 | -6.1402 | -6.674 | -6.7113

## Slide 41: Thank you

## Slide 42: References
[1] https://images.fineartamerica.com/images-medium-large-5/refraction-and-total-internal-reflection-russell-kightley.jpg
[2] https://www.youtube.com/watch?v=N_kA8EpCUQo
[3] P. Aithal and H. Ravindra, Textbook of Engineering Physics, 1st ed. Acme Learning Private Limited, 2021.
[4]W. Eickhoff and R. Ulrich, "Optical frequency domain reflectometry in single‐mode fiber", Applied Physics Letters, vol. 39, no. 9, pp. 693-695, 1981. Available: 10.1063/1.92872
[5]M. Froggatt and J. Moore, "High-spatial-resolution distributed strain measurement in optical fiber with Rayleigh scatter", Applied Optics, vol. 37, no. 10, p. 1735, 1998. Available: 10.1364/ao.37.001735.
[6] S. Loranger, M. Gagne, V. Lambin-Iezzi, and R. Kashyap, "Rayleigh scatter based order of magnitude increase in distributed temperature and strain sensing by simple UV exposure of optical fibre," Sci Rep, vol. 5, p. 11177, Jun 16 2015