## Slide 1: State of Charge Predication of Lithium-ion batteries
Sahana Upadhya
Lukas Desorcy
Mike Wagner
Allison Mahvi

## Slide 2
Depends
Battery degradation model
Number of cycles
Starting and ending SOC of the half-cycles
on
Aging of the battery over time due to all processes that lead to degradation other than cycling
Calendar aging
Rest SOC
Temperature
State of Charge (SOC)
Depth of Discharge (DOD)
Number of cycles
Cyclic aging
Degradation of the battery with every cycle of charging and discharging.
Battery Degradation Model
Validate model through testing:
Cyclic testing
  Aging
  Use case SOC estimation
Relaxation tests – rest case SOC estimation

## Slide 3
SOC is a measurement of the amount of energy in a battery expressed in percentage.
State of Charge (SOC)
VOLTAGE  Simplest estimation of SOC
transfer
Charging
Potential Difference
Voltage
Energy
SOC
Discharging
Potential Difference
Voltage
Energy
SOC

## Slide 4
Therefore, voltage changes with time
Rest
Concentration gradient in electrode of li-ion battery
Equalizes
Time
Internal resistance depends on many parameters like time, SOC, SOH
Voltage
Terminal Voltage
Internal Resistance
SOC
Voltage
SOC – Voltage relationship not parallel  Complex

## Slide 5
Accurate Estimation of State of Charge
Used in
Transport application
Lithium batteries
Variability in drive cycles and operational profiles
Accurate assessment of available energy
High precision estimation of SoC
Safety, reliability and endurance
Improved energy management
Maximized usage and planning

## Slide 6
Equipment
SOC prediction with use
SOC prediction at rest
Cyclic tester
Battery Management software
Thermal Chamber
Cyclic testing of the battery
Data processed
Collaboration with two other teams to develop physics-based model and machine learning models
Relaxation tests at varying SOC
Develop a relationship between various parameters and the relaxation curve
Predict the relaxation curve

## Slide 7
Digatron – Lithium Cell Tester
Cyclic testing – Charging, Discharging, Rest
Data acquisition rate – 2 ms per circuit
21 circuits with different current – voltage capabilities.
Current – Voltage capabilities
  0.25 – 100 A 0 - 18 V
  1000 A 5 V
  0.1 – 100 A 5 – 100 V

## Slide 8
Battery Management Software
Write intricate test programs.
Register required data – voltage, current, Ah, temp – at desired frequency
Monitor tests in progress
Generate basic graphs
Store battery characteristic data

## Slide 9
Thermal Chamber
Controls Ambient temperature when performing tests.
Provides a protected environment to perform tests – fire safety features.
Temperature range: -45 ℃ to 190℃.

## Slide 10
Battery Details
Parameter | 
Cell geometry | Pouch
Anode Material | 
Cathode Material | Graphite
Electrolyte | 
OCV of full cell (100% SOC) | 4.2 V
OCV of empty cell (0% SOC) | 2.75 V
Cell capacity | 5450 mAh
Parameter | 
Cell geometry | Pouch
Anode Material | 
Cathode Material | Graphite
Electrolyte | 
OCV of full cell (100% SOC) | 4.2 V
OCV of empty cell (0% SOC) | 2.75 V
Cell capacity | 5450 mAh
Thermocouples
Battery Fixture

## Slide 11
Cyclic testing
Step | Operator | Nominal Value | Limit | Action | Registration
1 | SET | Rlevel = 3 | > 4.2 V < 3 V > 60 C1 | ERR 2 ERR 2 ERR 2 | STANDARD
2 | BEG |  |  |  | 1 sec
3 | DCH | 21.8 A | < 3.01 V |  | 1 sec
4 | CHA | 21.8 A 4.1 V | 5 sec & < 0.545 A |  | 1 sec
5 | PAU |  | 30 sec |  | 1 sec
6 | CYC | 20* |  |  | 
Cyclic testing at 1C, 2C, 3C, 4C – 50 cycles
Data Collected:
Current
Voltage
Electric Charge (Ah)
Temperature (four thermocouples)
These tests very performed at ambient temperature
C-rate is the rate at which current is supplied to fully charge a battery.
1C – 1 hour to fully charge battery. 4C – ¼ hr = 15 min to fully charge the battery

## Slide 12
- Top
- Edge
- Bottom
- Side edge

## Slide 13
Cyclic data used to calibrate physics-based model
Physics-based model used to generate accurate cell performance data
Experimental data
+
Physics-based model data
Train Machine Learning model

## Slide 14
Physics based model
The physics-based modeling approach can simulate the electrochemical and intrinsic dynamic behavior of a cell.
Experimental data is used to calibrate the battery
Characterized through 5 main Partial Differential Equations  developed in GT-AutoLion (li-ion simulation software)

## Slide 15
Step 1 - C/20 test
Cathode capacity loading
Cathode thickness
Step 3 – Refining
Match experimental Open-circuit Voltage
N/P ratio
Initial SoC
Anode thickness
Separator thickness
Match SOC
Anode and Cathode particle size
Heat transfer coefficient
Step 2
1C-4C test
Cathode loading: Capacity of cathode per unit area of the cathode.
N/P ratio This relates to amount of active material in each electrode

## Slide 16
10 cycles at 1C C-rate
Predicted SoC values for the last 10 cycles of each C-rate
A combination of physics-based modelling and ML may prove valuable for longer test programs and State of health analysis and testing
Predicts SOC within 1-2% root-mean-square-error (RMSE)
Predicts SOC within 1% RMSE
Physics-based model
Feed forward neural network model

## Slide 17: Relaxation Tests
Identifying a correlation between open-circuit voltage, SOC and relaxation time required to achieve the stabalized OCV

## Slide 18: Relaxation time
Battery takes time to stabilize and reach a final stable Open Circuit Voltage (OCV).
Voltage Drop – Change in current
Forced regime – Current not equal to 0
Relaxation – No current battery stabilization
Voltage Drop
Voltage Drop
Forced Regime
Relaxation
Notes: Graph taken from our experimental data
Shows voltage behavior with change in current value

## Slide 19
D
B
C
E
F
An approximate error of 4% SOC introduced for a difference in 2 mV
If a 24 hr OCV value is used to find SOC on a 1 hr OCV vs SOC curve
C  OCV measured after 24 hr of relaxation
D  Same OCV on a 1 hr relaxation curve
E  Over-estimation of SOC
F  Actual SOC value
Li, An, et al. "Fast characterization method for modeling battery relaxation voltage." Batteries 2.2 (2016): 7.
Notes: This slide demonstrates how a small deviation in OCV results in an error in SOC.
The first graph shows a relaxation curve.
The OCV at point C – after 24 hour relaxation is taken as the OCV
OCV_C is used as the OCV to find the corresponding SOC on a 1hour relaxation time graph as seen in graph two.
This results in an over-estimation of the SOC value.
The realistic value of SOC will be found by taking the OCV at point B – after 1 hour of relaxation of the battery - and using this value as the OCV in a 1 hour relaxation time graph of OCV vs SOC (shown in graph 2 as point B)
The third graph further highlights the same fact:
  C  OCV measured after 24 hr of relaxation
  D  Same OCV on a 1 hr relaxation curve
  E  Over-estimation of SOC
  F  Actual SOC value
  Taken from literature – test conducted on a Li-ion battery LiFePO4

## Slide 20
Relaxation time and Battery History
OCV measured for different SOCs after different relaxation periods after charge and after discharge
Relaxation time
OCV approaches stable value
Battery History plays a role in relaxation characteristics.
Li, An, et al. "Fast characterization method for modeling battery relaxation voltage." Batteries 2.2 (2016): 7.
Notes: Taken from literature to shows that history and relaxation time effects the stabilizing of the battery to a steady OCV
Charging to a s specific SOC and discharging to the specific SOC effects the relaxation in different ways and we see the charge and discharge values approaching with increased relaxation time.
Taken from literature – test conducted on a Li-ion battery LiFePO4

## Slide 21
Voltage at any stage of relaxation can be related to an accurate SOC
Objective
Develop correlation between relaxation curve and SOC
20 min
1 hr
Identify parameters that effect the relaxation curve

## Slide 22
C-rate – 1C, 2C, 3C, 4C
Temperature – 20℃, 30℃, 40℃
Start and End SOC
Capacity charge/discharge
Charge/discharge
State of Health
- Rate at which current is supplied
- Energy entering/leaving the battery
Parameters
- Effects of battery degradation
Notes: Therefore, we have chosen the following parameters to test and analyze their relationship to the relaxation curve

## Slide 23
Initial Test Plan
Chart: Time
Chart: Time
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16
SOC | 100 | 95 | 95 | 95 | 95 | 90 | 90 | 90 | 90 | 85 | 85 | 85 | 85
Charge to 100%
Discharge by 5%
Relax for 10 hours
C-rate: 1C and 4C
Temperature: 20 ℃
1C and 4C test performed on two different batteries

## Slide 24
Step wise discharge and relaxation

## Slide 25
Time taken for voltage to stabilize

## Slide 26
Two different batteries were used. The capacity of both the batteries are slightly different
Final voltage for higher C-rate higher – especially for higher SOC
Will it converge if allowed to rest for longer?
Voltage drop larger
Battery stabilizes

## Slide 27
95
90
85
80
75
70
65
60
55
50
45
40
35
30
25
20
15
10
5
10 hours
Relaxation begins
Relaxation ends
For each point i during the relaxation
For each SOC relaxation curve
Analyzing the time taken to reach fully relaxed voltage
SOC

## Slide 28
Next Steps
Perform the same test again to see if the relaxation behavior is repeatable.
Perform similar tests for the remaining SOCs.
Attempt to find a correlation between various parameters and voltage at various stages of relaxation.
Use physics-based model to predict the relaxation curve and therefore estimate the accurate SOC.
Perform further cyclic testing for state of health analysis and study aging mechanisms.

## Slide 29
Thank You

## Slide 30
D
B
C
E
F
C  OCV measured after 24 hr of relaxation
D  Same OCV on a 1 hr relaxation curve
E  Over-estimation of SOC
F  Actual SOC value
Notes: If you think slide 4 is too cluttered and should be spaced into two slides

## Slide 31
An approximate error of 4% SOC introduced for a difference in 2 mV
If a 24 hr OCV value is used to find SOC on a 1 hr OCV vs SOC curve
Notes: If you think slide 4 is too cluttered and should be spaced into two slides

## Slide 32
20C
30C
40C
Test Plan
1C
2C
3C
4C
100% SOC – 80% SOC  1% discharge intervals  Relax  20 relaxations
80% SOC – 20% SOC  10% discharge intervals  Relax  6 relaxations
20% SOC – 0% SOC  1% discharge intervals  Relax  20 relaxations
552 relaxations curves
C-rate
Temperature
End SOC
1104 relaxations curves
Charge and discharge
Time required to test all these combinations:
10 min relaxation – 10 days
24 hours relaxation – 1250 days
Notes: Basic test plan varying the initial test parameters.
Time required to complete it is too long
Plan to use design of experiment to reduce the number of tests required.