TYPE 73: FUEL CELL STACK

General Description

This component models a fuel cell stack with a proton exchange membrane for five different input modes, where four of the modes are based on the same equation.  The different modes allow the user to choose the mode that fits the amount of data available for the fuel cell stack.  The fuel cell stack can have either voltage or current as input.  A switch can turn the fuel cell off or on.

Nomenclature

a	-	Constant for Temperature-Voltage equation (diffusion)

A	-	Outside area of the fuel cell

b	-	Constant for Temperature-Voltage equation (migration)

Cmass	-	Average heat capacity for the fuel cell* Mass of the fuel cell

c	-	Constant for Temperature-Voltage equation (migration)

cO2	-	Concentration of oxygen

E	-	Reversible voltage

	-	Parameters for the activation voltage loss

	-	Parameters for the resistance voltage loss

I	-	Current through the fuel cell

Ihigh	-	Maximal current for high temp I-V curve

Ilow	-	Maximal current for low temp I-V curve

Itemp	-	Maximal current at the given temperature

k	-	Constant for Temperature-Voltage equation (diffusion)

lud	-	Logical number of data file

mH2	-	H2-mass flow to the fuel cell

nfuel	-	Fuel cell number in data file

act	-	Activation voltage loss

eff	-	Total efficiency of fuel cell

el	-	Voltage efficiency of fuel cell

ohmic	-	Voltage loss due to resistance

Pel	-	Electric power from the fuel cell

PH2	-	Partial pressure of hydrogen

Pmax	-	Maximal power output of the fuel cell

PO2	-	Partial pressure of oxygen

Pref	-	Reference output of the fuel cell (output the data are given for).

puse0	-	Power consumption of fuel cell when not in use

puse1	-	Power consumption of fuel cell  when in use

q	-	Total heat production in the fuel cell per time

qrem 	-	Heat that has to be removed to prevent overheating of the fuel cell

qsur	-	Heat loss to the surroundings

qheat	-	Heat loss to heat up the fuel cell

R	-	Internal resistance of the fuel cell

Tsur	-	Temperature of the surroundings of the fuel cell

Tstart	-	Initial temperature of fuel cell

Tfc	-	Temperature of fuel cell

Thigh	-	Temperature for high temp I-V curve

Tlow	-	Temperature for low temp I-V curve

Uoc	-	Open circuit voltage for fuel cell (I=0.0)

Ufc	-	Voltage over fuel cell

Uloss	-	Heat loss coefficient for the fuel cell

Ulow	-	Maximal current for low temp I-V curve

Uhigh	-	Maximal current for high temp I-V curve

Utemp	-	Maximal voltage at the given temperature

Utn	-	Thermo-neutral voltage

ybz	-	Control function (0.0-1.0, where 0.0=off and 1.0=on)

zs	-	number of cell in series

Mathematical Description

This subroutine models a fuel cell stack with a proton exchange membrane after /1/.  The equation for the I-V curve for one specific temperature is for mode 1, 3, 4 and 5:

1

(mode 4: a and k is zero)

The current for the high and the low temperature curve is calculated from this equation.  To find the current at the working temperature of the fuel cell, the current is calculated by linear interpolation:

2

Mode 2 models a fuel cell stack with a proton exchange membrane after /2/ and /3/. The equation for the I-V curve is:

where

The calculations are done by iterations.  When the temperature of the fuel cell reaches maximum allowed temperature, heat has to be removed from the fuel cell to not exceed the maximal temperature. To do this, the efficiencies of the fuel cell has to be calculated:

Two main efficiencies are calculated, the electric efficiency and the total efficiency.  The reason for calculating two efficiencies is that it is only the electric efficiency that will heat up the electrolyzer.  The total efficiency also includes the loss of hydrogen that will not heat up the fuel cell (the electric efficiency and the total efficiency will be very close at normal or high production, but will differ at a very low production rate).

3

4

The new temperature of the fuel cell is based on the temperature from the last time step and is calculated from heat produced and energy lost to the environment:

5

6

7

The heat loss factor and the heat capacity of the fuel cell should be an average of the whole fuel cell system that will be heated by the operation of the fuel cell.

The heat that has to be removed is:

8

The used mass of hydrogen is calculated by:

TRNSYS Component Configuration

PARAMETER NO.			DESCRIPTION

1 	zs	-	number of cell in series

2	Ar	-	Area of each cell

3	V0	-	Minimal voltage for reaction to occur

4	Vloss	-	Heat loss coefficient of fuel cell

5 	Tsur	-	Surrounding temperature

6 	Tstart	-	Initial temperature of fuel cell

7 	lud	-	Logical number of data file

8 	nfuel	-	Fuel cell number in data file

INPUT NO.			DESCRIPTION

1	mofc	-	Mode for calculations

0 = Current is calculated

1 = Voltage is calculated

2	Vfc	-	Voltage over the fuel cell

or

Ifc	-	Current through the fuel cell

3	yfc	-	Control function (Switch)

OUTPUT NO.			DESCRIPTION

1	Vfc	-	Voltage over fuel cell

2	Ifc	-	Current through the fuel cell

3	Pel 	-	Electric power from the fuel cell

4	fc	-	Power efficiency (voltage efficiency)

5	mH2	-	H2-mass flow to the fuel cell

6	Tfc	-	Temperature of the fuel cell

7	qrem	-	Heat that has to be removed to prevent overheating of the fuel cell per time

8	q	-	Total heat produced by the fuel cell per time

9	qsur	-	Heat loss to the surroundings per time

10	qheat	-	Heat loss to heat up the fuel cell per time

11	Puse0	-	Power consumption of fuel cell when not in use

12	Puse1	-	Power consumption of fuel cell when in use

13	Ifcvmax	-	Maximal current allowed through the fuel cell (at operating temperature)

Informational Flow Diagrams

Data file input

The data for a fuel cell has to be given in a separate file. The first line in this file will give the number of fuel cells given in the file. The data for each different cell will have two lines; the first line will give the number of the cell in the file, the second line will give the data for the cell.  There are several different modes for the fuel cell, and each requires different data.  The data for the different modes can look like this (the third line (P1-P23) should not be in the file, but are included here to show what the data represents):

# Mode 1

4,Fuel cell Tor

1   20 0.00019 0.045 0.1 0.0001 0.001 80 0.000103 0.03 0.1 0.0001 0.001 1.36 62500 80  62.5 344 1500 2500 0. 0.01 10

P1 P2   P3         P4    P5   P6      P7      P8    P9        P10 P11   P12    P13   P14  P15   P16 P17  P18 P19  P20 P21 P22 P23

P1 = mode	:	Mode for data input =1

P2 = LT	:	Temperature of Low-Temperature I-V-curve for fuel cell [C]

P3 = Rlt	:	Resistance in the fuel cell at low temperature times cell area [Ohm*m2]

P4 = blt	:	Parameter for migration in fuel cell at low temperature [V]

P5 = clt	:	Parameter for migration in fuel cell at low temperature [m2/A]

P6 = alt	:	Parameter for diffusion in fuel cell at low temperature [V]

P7 = klt	:	Parameter for diffusion in fuel cell at low temperature [m2/A]

P8 = HT	:	Temperature of High-Temperature I-V-curve for fuel cell [C]

P9 = Rht	:	Resistance in the fuel cell at high temperature times cell area [Ohm* m2]

P10 = bht	:	Parameter for migration in fuel cell at high temperature [V]

P11 = cht	:	Parameter for migration in fuel cell at high temperature per cell area [m2/A]

P12 = aht	:	Parameter diffusion in fuel cell at high temperature [V]

P13 = kht	:	Parameter diffusion in fuel cell at high temperature [m2/A]

P14 = Area	:	Area of the surface of the fuel cell per cell area and cell [m2/ m2].  This number is sized by in the power of 2/3, so it assumes a cube formed fuel cell!

P15= Cmass	:	Heat capacity of fuel cell [J/K]

P16= Thmax	:	Maximum operating temperature of fuel cell[C]

P17= Puse0	:	Power consumption of fuel cell when the fuel cell is not used per cell area and cell [W/ m2]

P18= Puse1	:	Power consumption of fuel cell when the fuel cell is used per cell area and cell    [W/ m2]

P19= Ifcmlt	:	Maximum allowed current at low temperature per cell area [A/ m2]

P20= Ifcmht	:	Maximum allowed current at high temperature per cell area [A/ m2]

P21= curloss	:	Loss of current in fuel cell (Current that passes through the fuel cell without producing hydrogen) per cell area [A/(V*m2)]

P22= hydloss	:	Loss of hydrogen over to the oxygen side in percent related to production at minimum allowed current

P23= Ifcmin	:	Minimum allowed current per cell area [A/m2]

OUTPUT to the listing file will look like this:

Parameter from file to fuel cell, unit 37:

mode = 1

lt     =  2.0000E+01  Rlt    =  1.9000E-04  blt    =  4.5000E-02

clt    =  1.0000E-01  alt    =  1.0000E-04  klt    =  1.0000E-03

ht     =  8.0000E+01  Rht    =  1.0300E-04  bht    =  3.0000E-02

cht    =  1.0000E-01  aht    =  1.0000E-04  kht    =  1.0000E-03

area   =  1.3600E+00  cmass  =  6.2500E+04  thmax  =  8.0000E+01

puse0  =  6.2500E+01  puse1  =  3.4400E+02  Ifcmlt =  1.5000E+03

Ifcmht =  2.5000E+03  curloss=  0.0000E+00  hydloss=  1.0000E-02

Ifcmin =  1.0000E+01

# Mode 2

5,Fuel cell Odin

2 -0.9514 0.004109 7.4e-5 -0.000187 8.115e-5 -1.77e-7 2.045e-9 1 0.21 0.015 40000 80  0    0    6000 7000 0. 0.01 100

P1  P2      P3           P4        P5            P6             P7      P8        P9 P10   P11    P12  P13 P14 P15 P16 P17  P18 P19 P20

P1 = mode	:	Mode for data input =2

P1 = 1	:	Parameter for activation voltage drop

P3 = 2	:	Parameter for activation voltage drop

P4 = 3	:	Parameter for activation voltage drop

P5 = 	:	Parameter for activation voltage drop

P6 = 1	:	Parameter for resistance voltage drop

P7 = 2	:	Parameter for resistance voltage drop

P8 = 3	:	Parameter for resistance voltage drop

P9 = pH2	:	Partial pressure of H2 [atm]

P10 = pO2	:	Partial pressure of O2 [atm]

P11 = Area	:	Area of the surface of the fuel cell per cell area and cell [m2/ m2].  This number is sized by in the power of 2/3, so it assumes a cube formed fuel cell!

P12= Cmass	:	Heat capacity of fuel cell [J/K]

P13= Thmax	:	Maximum operating temperature of fuel cell[C]

P14= Puse0	:	Power consumption of fuel cell when the fuel cell is not used per cell area and cell [W/ m2]

P15= Puse1	:	Power consumption of fuel cell when the fuel cell is used per cell area and cell    [W/ m2]

P16= Ifcmlt	:	Maximum allowed current at low temperature per cell area [A/ m2]

P17= Ifcmht	:	Maximum allowed current at high temperature per cell area [A/ m2]

P18= curloss	:	Loss of current in fuel cell (Current that passes through the fuel cell without producing hydrogen) per cell area [A/(V*m2)]

P19= hydloss	:	Loss of hydrogen over to the oxygen side in percent related to production at minimum allowed current

P20= Ifcmin	:	Minimum allowed current per cell area [A/m2]

OUTPUT to the listing file will look like this:

Parameter from file to fuel cell, unit 37:

mode = 2

eps1   = -9.5140E-01  eps2   =  4.1090E-03  eps3   =  7.4000E-05

eps4   = -1.8700E-04  gam1   =  8.1150E-05  gam2   = -1.7700E-07

gam3   =  2.0450E-09  pH2    =  1.0000E+00  pO2    =  2.1000E-01

area   =  1.5000E-02  cmass  =  4.0000E+04  thmax  =  8.0000E+01

puse0  =  0.0000E+00  puse1  =  0.0000E+00  Ifcmlt =  6.0000E+03

Ifcmht =  7.0000E+03  curloss=  0.0000E+00  hydloss=  1.0000E-02

Ifcmin =  1.0000E+02

# Mode 3

2,Fuel cell Gudrun

3   20 1000 0.787 3000 0.428 80 2000 0.776 5000 0.490 0.015 40000 80 0      0    3000 5000 0.  0.01 100

P1 P2   P3     P4    P5   P6      P7   P8    P9     P10  P11   P12    P13   P14 P15 P16 P17  P18 P19 P20  P21

P1 = mode	:	Mode for data input =3

P2 = LT	:	Temperature of Low-Temperature I-V-curve for fuel cell [C]

P3 = I1	:	Current density for first point of low temperature curve [A/m2]

P4 = V1	:	Voltage at low temperature and current=I1 [V]

P5 = I2	:	Current density for maximum power point of low temperature curve [A/m2]

P6 = V2	:	Voltage at maximum power point at low temperature [V]

P7 = HT	:	Temperature of High-Temperature I-V-curve for fuel cell [C]

P8 = I3	:	Current density for first point of high temperature curve [A/m2]

P9 = V3	:	Voltage at high temperature and current=I3 [V]

P10 = I4	:	Current density for maximum power point of high temperature curve [A/m2]

P11 = V4	:	Voltage at maximum power point at high temperature [V]

P12 = Area	:	Area of the surface of the fuel cell per cell area and cell [m2/ m2].  This number is sized by in the power of 2/3, so it assumes a cube formed fuel cell!

P13= Cmass	:	Heat capacity of fuel cell [J/K]

P14= Thmax	:	Maximum operating temperature of fuel cell[C]

P15= Puse0	:	Power consumption of fuel cell when the fuel cell is not used per cell area and cell [W/ m2]

P16= Puse1	:	Power consumption of fuel cell when the fuel cell is used per cell area and cell    [W/ m2]

P17= Ifcmlt	:	Maximum allowed current at low temperature per cell area [A/ m2]

P18= Ifcmht	:	Maximum allowed current at high temperature per cell area [A/ m2]

P19= curloss	:	Loss of current in fuel cell (Current that passes through the fuel cell without producing hydrogen) per cell area [A/(V*m2)]

P20= hydloss	:	Loss of hydrogen over to the oxygen side in percent related to production at minimum allowed current

P21= Ifcmin	:	Minimum allowed current per cell area [A/m2]

OUTPUT to the listing file will look like this:

# Parameter from file to fuel cell, unit 37:

# mode = 3

# Temp1  =  2.0000E+01  I1     =  1.0000E+03  V1     =  7.8700E-01

# I2     =  3.0000E+03  V2     =  4.2800E-01  Temp2  =  8.0000E+01

# I3     =  2.0000E+03  V3     =  7.7600E-01  I4     =  5.0000E+03

# V4     =  4.9000E-01  area   =  1.5000E-02  cmass  =  4.0000E+04

# thmax  =  8.0000E+01  puse0  =  0.0000E+00  puse1  =  0.0000E+00

# Ifcmlt =  3.0000E+03  Ifcmht =  5.0000E+03  curloss=  0.0000E+00

# hydloss=  1.0000E-02  Ifcmin =  1.0000E+02

# Parameter calculated from the given I-V points for the equation:

# T[C],I[A/m2],V[V]

# V=V0-(b0+b1*T)*log(I+1)-(r0+r1*T)*I-(a0+a1*T)*(exp((k0+k1*T)*I)-1)

# b0=  4.5496E-02  r0=  1.8057E-04  a0= -5.9018E-07  k0= -5.2677E-04

# b1= -1.7764E-04  r1= -1.2046E-06  a1=  2.9509E-08  k1=  2.6339E-05

# Mode 4

3,Fuel cell Froy

4 20 1750 0.68 80 1750 0.68 0.015 40000 80    0     0     6000 7000 0.   0.01 100

P1 P2 P3   P4  P5   P6    P7    P8      P9    P10 P11   P12 P13    P14 P15 P16 P17

P1 = mode	:	Mode for data input =3

P2 = LT	:	Temperature of Low-Temperature I-V-curve for fuel cell [C]

P3 = I1	:	Current density for maximum power point of low temperature curve [A/m2]

P4 = V1	:	Voltage at maximum power point at low temperature [V]

P5 = HT	:	Temperature of High-Temperature I-V-curve for fuel cell [C]

P6 = I2	:	Current density for maximum power point of high temperature curve [A/m2]

P7 = V2	:	Voltage at maximum power point at high temperature [V]

P8 = Area	:	Area of the surface of the fuel cell per cell area and cell [m2/ m2].  This number is sized by in the power of 2/3, so it assumes a cube formed fuel cell!

P9= Cmass	:	Heat capacity of fuel cell [J/K]

P10= Thmax	:	Maximum operating temperature of fuel cell[C]

P11= Puse0	:	Power consumption of fuel cell when the fuel cell is not used per cell area and cell [W/ m2]

P12= Puse1	:	Power consumption of fuel cell when the fuel cell is used per cell area and cell    [W/ m2]

P13= Ifcmlt	:	Maximum allowed current at low temperature per cell area [A/ m2]

P14= Ifcmht	:	Maximum allowed current at high temperature per cell area [A/ m2]

P15= curloss	:	Loss of current in fuel cell (Current that passes through the fuel cell without producing hydrogen) per cell area [A/(V*m2)]

P16= hydloss	:	Loss of hydrogen over to the oxygen side in percent related to production at minimum allowed current

P17= Ifcmin	:	Minimum allowed current per cell area [A/m2]

OUTPUT to the listing file will look like this:

Parameter from file to fuel cell, unit 37:

mode = 4

Temp1  =  2.0000E+01  I1     =  1.7500E+03  V1     =  6.8000E-01

Temp2  =  8.0000E+01  I2     =  1.7500E+03  V2     =  6.8000E-01

area   =  1.5000E-02  cmass  =  4.0000E+04  thmax  =  8.0000E+01

puse0  =  0.0000E+00  puse1  =  0.0000E+00  Ifcmlt =  6.0000E+03

Ifcmht =  7.0000E+03  curloss=  0.0000E+00  hydloss=  1.0000E-02

Ifcmin =  1.0000E+02

Parameter calculated from the given I-V points for the equation:

T[C],I[A/m2],V[V]

V=V0-(b0+b1*T)*log(I+1)-(r0+r1*T)*I

b0= -1.6967E-02  b1= -1.3141E-04  r0=  3.9826E-04  r1=  7.5046E-08

# Mode 5

4, Fuel cell Balder

5   80 2000 0.74 6000 0.52 8700 0  80 2000 0.74 6000 0.52 8700 0   0.015 40000 80   0     0   6000  7000 0.  0.01 100

P1 P2   P3    P4    P5   P6     P7  P8 P9  P10  P11   P12  P1  P14 P15 P16    P17   P18 P19 P20  P21   P22 P23 P24 P25

P1 = mode	:	Mode for data input =3

P2 = LT	:	Temperature of Low-Temperature I-V-curve for fuel cell [C]

P3 = I1	:	Current density for first point of low temperature curve [A/m2]

P4 = V1	:	Voltage at low temperature and current=I1 [V]

P5 = I2	:	Current density for maximum power point of low temperature curve [A/m2]

P6 = V2	:	Voltage at maximum power point at low temperature [V]

P7 = I3	:	Current density for current beyond maximum power point of low temperature curve [A/m2]

P8 = V3	:	Voltage at low temperature and current=I3 [V]

P9 = HT	:	Temperature of High-Temperature I-V-curve for fuel cell [C]

P10 = I4	:	Current density for first point of high temperature curve [A/m2]

P11= V4	:	Voltage at high temperature and current=I4 [V]

P12 = I5	:	Current density for maximum power point of high temperature curve [A/m2]

P13 = V5	:	Voltage at maximum power point at high temperature [V]

P14= I6	:	Current density for current beyond maximum power point of high temperature curve [A/m2]

P15= V6	:	Voltage at high temperature and current=I6 [V]

P16 = Area	:	Area of the surface of the fuel cell per cell area and cell [m2/ m2].  This number is sized by in the power of 2/3, so it assumes a cube formed fuel cell!

P17= Cmass	:	Heat capacity of fuel cell [J/K]

P18= Thmax	:	Maximum operating temperature of fuel cell[C]

P19= Puse0	:	Power consumption of fuel cell when the fuel cell is not used per cell area and cell [W/ m2]

P20= Puse1	:	Power consumption of fuel cell when the fuel cell is used per cell area and cell    [W/ m2]

P21= Ifcmlt	:	Maximum allowed current at low temperature per cell area [A/ m2]

P22= Ifcmht	:	Maximum allowed current at high temperature per cell area [A/ m2]

P23= curloss	:	Loss of current in fuel cell (Current that passes through the fuel cell without producing hydrogen) per cell area [A/(V*m2)]

P24= hydloss	:	Loss of hydrogen over to the oxygen side in percent related to production at minimum allowed current

P25= Ifcmin	:	Minimum allowed current per cell area [A/m2]

OUTPUT to the listing file will look like this:

# Parameter from file to fuel cell, unit 37:

# mode = 5

# Temp1  =  8.0000E+01  I1     =  2.0000E+03  V1     =  7.4000E-01

# I2     =  6.0000E+03  V2     =  5.2000E-01  I3     =  8.7000E+03

# V3     =  0.0000E+00  Temp2  =  8.0000E+01  I4     =  2.0000E+03

# V4     =  7.4000E-01  I5     =  6.0000E+03  V5     =  5.2000E-01

# I6     =  8.7000E+03  V6     =  0.0000E+00  area   =  1.5000E-02

# cmass  =  4.0000E+04  thmax  =  8.0000E+01  puse0  =  0.0000E+00

# puse1  =  0.0000E+00  Ifcmlt =  6.0000E+03  Ifcmht =  7.0000E+03

# curloss=  0.0000E+00  hydloss=  1.0000E-02  Ifcmin =  1.0000E+02

# Parameter calculated from the given I-V points for the equation:

# T[C],I[A/m2],V[V]

# V=V0-(b0+b1*T)*log(I+1)-(r0+r1*T)*I-(a0+a1*T)*(exp((k0+k1*T)*I)-1)

# b0=  5.2016E-02  r0=  2.1461E-05  a0=  1.3339E-03  k0=  6.8703E-04

# b1=  0.0000E+00  r1=  0.0000E+00  a1=  0.0000E+00  k1=  0.0000E+00

References

/1/  Chamberlin, C.E., Lehman, P.A., Reid, R.M. Herron, T.G.  Preliminary results of the Schatz fuel cell project.  In: Hydrogen Energy progress X, Proceedings of the 10th world hydrogen energy conference, editors D.L.Block aand T.N. Veziroglu,  1994.

/2/ Amplett, J.C., R.M. Baumert, R.F. Mann, B.A.Peppley, P.R. Roberge and T.J. Harris. Performance Modeling of the Ballard MarkIV Solid Polymer Electrolyte Fuel Cell, I. Mechanistic Model development.  In: J. Electrochem. Soc. Vol. 142, No.1 pp1-8, 1995.

/3/ Amplett, J.C., R.M. Baumert, R.F. Mann, B.A.Peppley, P.R. Roberge and T.J. Harris.  Performance Modeling of the Ballard MarkIV Solid Polymer Electrolyte Fuel Cell, II. Empirical Model development.  In: J. Electrochem. Soc. Vol. 142, No.1 pp9-15, 1995.